KUANGSHUN Liquid photoimageable solder mask

（Data Sheet KSM-S6188）

KSM-S6188 is photoimageable solder mask. It is two-component and screen printing type with good screen printing adaptability, good allowance of pre-drying and developing. The post cured film provides excellent adhesion, high hardness, resistance to chemicals and heat.

一、Type of Ink：

| Type of Base | Color |  | Type of hardener |  |  | Main features |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| KSM-S6188 G1 | Light green（incline to yellow） |  | KSM-18 |  |  | High gloss, pre-baking allowance and good resistance to heat. |  |
| KSM-S6188 G2 |  | Medium green（incline to yellow） |  |  |  |  |  |
| KSM-S6188 G3 |  | Deep green（incline to blue） |  |  |  |  |  |
| KSM-S6188 G4 |  | Medium green（incline to yellow） |  |  |  |  |  |
| KSM-S6188 G5 | Medium green（incline to blue） |  | KSM-18 A1 |  |  | Small shrinkage, good resistance to heat and chemicals. Suit for the production of thick copper-boards and tin-boards. |  |
| KSM-S6188 G6 |  | Medium green（incline to yellow） |  |  |  |  |  |
| KSM-S6188 G9 |  | Light green（incline to blue） |  |  |  |  |  |
| KSM-S6188 BL |  | Blue |  |  |  |  |  |
| KSM-S6188 BK |  | Black |  |  |  |  |  |
| KSM-S6188 R |  | Red |  |  |  |  |  |
| KSM-S6188 RD | Deep red |  | KSM-18 A3 |  |  | Small under-cut, suit for the production of 3mil solder-dam. |  |
| KSM-S6188 Y |  | Yellow |  |  |  |  |  |
| KSM-S6188 W |  | White |  |  |  |  |  |
| KSM-S6188 V |  | Violet red |  |  |  |  |  |
| KSM-S6188 EG2 |  | Medium green， no halogen（incline to yellow） |  |  |  |  |  |
| KSM-S6188 EG5 |  | Medium green， no halogen（incline to blue） |  |  |  |  |  |
| KSM-S6188 EG9 | Medium green ，no halogen（incline to blue） |  | KSM-18 A6 |  |  | High gloss and small under-cut, suit for the production of 3mil solder-dam, good resistance to heat and chemicals. |  |
| KSM-S6188 GA |  | Medium green and matt（incline to yellow） |  |  |  |  |  |
| KSM-S6188 GB |  | Medium green and matt（incline to blue） |  |  |  |  |  |
| KSM-S6188 GC |  | Medium green and matt（incline to yellow） |  |  |  |  |  |
| KSM-S6188 BKM |  | Black and matt |  |  |  |  |  |

二、Properties of Ink：

| Items | Features | Notes |
| --- | --- | --- |
| Color | Green, Blue, Yellow, Red, Black, White | About 40 |
| Fineness | ≤8μm | 0~25μm Fineness-of-Grind-Gages |
| Mixing ratio | Base/Hardener=3:1 | Weight ratio |
| Solid content after mixing | 75±3% |  |
| Viscosity after mixing（25℃） | 200±30 dPa·s | VT-04F |
| Density after mixing （25℃） | 1.20~1.40g/ml |  |
| Pot life after mixing | 24 hours | Store below 25 ℃ in dark |
| Environment standard | In compliance with ROSH directives | SGS testing |
| Pre-baking limit | 75℃, 70min |  |
| Exposure energy | 300~600mJ/cm2 | The effective value through the polyester film |
| Package | Main agent:750g,Hardener:250g |  |
| Shelf life | 6 months since the date of manufacture | Store below 25℃ in dark |

三、Properties of the film：

| Items | Features | Notes |
| --- | --- | --- |
| Pencil hardness | ≥6H | Pencil harder, JIS K5400 8.4 |
| Adhesion | 100/100 | Laceration experiment, JIS K5400 8.5 |
| Solvent resistance | good | 25℃, C2H5OH, 20min |
| Acid resistance | good | 25℃,10vol% H2SO4,20min |
| Alkali resistance | good | 25℃,10wt% NaOH,20min |
| Boiling water resistance | good | 100℃,30min |
| Insulation resistance | ≥1.0×1012Ω | IPC-SM-840C 3.8.2 |
| Endurance Voltage | 1000V DC/mil | IPC-TM650 |
| Resistance to molten solder | 260±5℃×10seconds×3times OK | JIS C6481 5.5 |
| Resistance to flame | UL94 V-0 | Certified number:UL-E189612 |
| Chemical-plating aurum | OK | Ni:5μm, Au:0.05μm |
| Electrical-plating aurum | OK | Ni:5μm, Au:1.0μm |

Attention:                                             
1.The main agent and hardener should be mixed according             
to the ratio and stirred thoroughly before using.               
2.We will offer you special diluent if the ink need to dilute.      
3.The values above are based on experiments in our lab. Experiments 
need to be carried out in order to get proper using condition.